[image: image1.png]&4 Master Wall Inc.



Aggre-flex EIFS – Continuously Insulated

Section 07 24 13

[image: image2.jpg]



Master Wall Guide Specification AF
Aggre-flex EIFS

PART I – GENERAL

1.01 SUMMARY
A. This document is to be used in preparing specifications for projects utilizing the Master Wall Inc.®  Aggre-flex Class PB (polymer-based) Exterior Insulation and Finish System (EIFS) designed to provide continuous insulation for the wall assembly.  Related Master Wall Inc.® documents:

1. Master Wall Inc.® Aggre-flex System Data Sheet

2. Master Wall Inc.® Aggre-flex System Application Instructions

3. Master Wall Inc.® Aggre-flex System Installation Details

4. Master Wall product data sheets

B. Related Sections

1. Unit Masonry – Section 04200

2. Concrete – Sections 03300 and 03400

3. Light Gauge Cold Formed Steel Framing – Section 05400

4. Wood Framing – Section 06100

5. Sealant – Section 07900

6. Flashing – Section 07600

1.02 SUBMITTALS

A. Manufacturer's specifications, details, installation instructions and product data

B. Manufacturer’s code compliance report 

C. Manufacturer's standard warranty

D. Applicator's industry training credentials

E. Samples for approval as directed by architect or owner

F. Sealant manufacturer's certificate of compliance with ASTM C 1382

G. Prepare and submit project-specific details (when required by contract documents)

1.03 REFERENCES

A. ASTM Standards:

ASTM B117 (Federal Test Standard 141A Method 6061) Standard Practice for Operating Salt Spray (Fog) 
Apparatus

ASTM C150 Standard Specification for Portland Cement

ASTM C297 Standard Test Method for Flatwise Tensile Strength of Sandwich Constructions

ASTM C578 Specification for Preformed Cellular Polystyrene Thermal Insulation

ASTM C1177 Standard Specification for Glass Mat Gypsum Substrate for Use as Sheathing

ASTM C1396 (formerly C 79) Standard Specification for Gypsum Board

ASTM D968 (Federal Test Standard 141A Method 6191) Standard Test Methods for Abrasion Resistance of 



Organic Coatings by Falling Abrasive

ASTM D1784 Specification for Rigid Poly (Vinyl Chloride) (PVC) and Chlorinated Poly (Vinyl Chloride) (CPVC) 



Compounds

ASTM D2247 (Federal Test Standard 141A Method 6201) Standard Practice for Testing Water Resistance of 



Coatings in 100% Relative Humidity

ASTM D3273 Standard Test Method for Resistance to Growth of Mold on the Surface of Interior Coatings in 



an Environmental Chamber

ASTM E84 Standard Test Method for Surface Burning Characteristics of Building Materials

ASTM E96 Test Methods for Water Vapor Transmission of Materials

ASTM E330 Test Method for Structural Performance of Exterior Windows, Doors and Curtain Walls by Uniform 



Static Air Pressure Difference

ASTM E331 Test Method for Water Penetration of Exterior Windows, Skylights, Doors and Curtain Walls by 



Uniform Static Air Pressure Difference.

ASTM E2098 Test Method for Determining Tensile Breaking Strength of Glass Fiber Reinforcing Mesh for Use 



in Class PB Exterior Insulation and Finish System after exposure to Sodium-Hydroxide 




Solution

ASTM E2134 Test Method for Evaluating the Tensile-Adhesion Performance of an Exterior Insulation and 



Finish System (EIFS)

ASTM E2178 Test Method for Air Permeance of Building Materials

ASTM E2357 Standard Test Method for Determining Air Leakage of Air Barrier Assemblies

ASTM E2485 (formerly EIMA Std. 101.01) Standard Test Method for Freeze-Thaw Resistance of Exterior 




Insulation and Finish Systems (EIFS) and Water-Resistive Barrier Coatings

ASTM E2486 (formerly EIMA Std. 101.86) Standard Test Method for Impact Resistance of Class PB and PI 



Exterior Insulation and Finish Systems (EIFS)

ASTM E2568 Standard Specification for Class PB Exterior Insulation and Finish Systems

ASTM G23 Standard Practice for Operating Light-Exposure Apparatus (Carbon-Arc Type) with and without 



Water for Exposure of Nonmetallic Materials

ASTM G53 Practice for Operating Light- and Water-Exposure Apparatus (Fluorescent UV-Condensation Type) 



for Exposure of Nonmetallic Materials

B. Building Code Standards

Acceptance Criteria for EIFS Clad Wall Assemblies
C. National Fire Protection Association (NFPA) Standards

NFPA 268 Standard Test Method for Determining Ignitibility of Exterior Wall Assemblies Using a Radiant Heat 



Energy Source

NFPA 285 Standard Method of Test for the Evaluation of Flammability Characteristics of Exterior Non-Load 



Bearing Wall Assemblies containing Combustible Components Using the Intermediate-Scale, 



Multistory Test Apparatus

D. Other Referenced Documents

American Association of Textile Chemists and Colorists AATCC-127 Water Resistance: Hydrostatic Pressure 



Test

APA Engineered Wood Association E30, Engineered Wood Construction Guide

UES Evaluation Report 433, Master Wall EIF Systems

1.04 SYSTEM DESCRIPTION

A. General: The Master Wall Inc.® Aggre-flex System is a continuously insulated (CI) Exterior Insulation and Finish System, Class PB (polymer-based), consisting of adhesive or mechanical fasteners, expanded polystyrene insulation board, base coat, reinforcing mesh(es) and finish.  The System shall be attached over an approved substrate and air/water barrier in accordance with the Aggre-flex application Details.  

B. Methods of Installation

1. Field Applied: The Aggre-flex System is applied to the substrate system in place.

2. Panelized: The Aggre-flex System is shop-applied to the prefabricated wall panels.
C. Design Requirements

1. Acceptable substrates for the Aggre-flex System shall be:

a. Exterior sheathing having a water-resistant core with fiberglass mat facers meeting ASTM C 1177.

b. Exterior fiber reinforced cement or calcium silicate boards.

c. APA Exterior or Exposure 1 Rated Plywood, Grade C-D or better, nominal 12.7 mm (1/2 in), minimum 4-
ply.
d. Unglazed, unpainted brick, cement plaster, concrete, or masonry.

e.  APA Exposure 1 rated Oriented Strand Board (OSB) or plywood, nominal 12.7 mm (1/2 in).
f.  Other substrates approved in writing from the manufacturer.
2. Deflection of substrate systems shall not exceed 1/240 times the span.

3. The substrate shall be flat within 6.4 mm (1/4 in) in a 3.05 m (10 ft) radius.

4. The slope of inclined surfaces shall not be less than 6:12, and the length shall not exceed 305 mm (12 in).

5. All areas requiring an impact resistance classification higher than “medium”, as defined by ASTM E 2486 (formerly EIMA Std. 101.86), shall be as detailed in the drawings and described in the contract documents.  

6. Expansion Joints

a. Design and location of expansion joints in the Aggre-flex System is the responsibility of the 
project designer and shall be noted on the project drawings.  As a minimum, expansion joints shall be 
placed at the following locations:
1) Where expansion joints occur in the substrate system.

2) Where building expansion joints occur.

3) At floor lines in wood frame construction (Reference Technical Bulletin #140).

4) At floor lines of non-wood framed buildings where significant movement is expected.

5) Where the Aggre-flex System abuts dissimilar materials.

6) Where the substrate type changes 

7) Where prefabricated panels abut one another

8) Where significant structural movement occurs such as changes in roofline, building shape or 
structural system.

7. Terminations

a. Interior foam expanding foam sealant may be required behind penetration openings.

b. The Aggre-flex System shall be held back from adjoining materials around openings and 
penetrations such as windows, doors and mechanical equipment a minimum of 12.7 mm (1/2 in) for 
sealant application.  Sealant joints shall be properly sized and designed for their anticipated 
movement (Reference Master Wall Inc.® Technical Bulletins #148 & 149).

c. The system shall be terminated a minimum of 152 mm (6 in) above finished grade.

d. Sealants

1) Shall be manufactured and supplied by others.

2) Shall be compatible with Aggre-flex System materials.  Refer to current Master Wall 
Inc.® Technical Bulletin #131 for listing of sealants approved by sealant manufacturer for use with 
EIFS.

3) The sealant backer rod shall be of closed cell.

8. Vapor Retarders and barriers – The use and location of vapor retarders and/or barriers within a wall 
assembly is the responsibility of the project designer and shall comply with local building code 
requirements. 

9. Dark Colors - The use of dark colors must be considered in relation to wall surface temperature as a 
function of local climatic conditions.  Use of dark colors in high temperature climates can affect the 
performance of the system.

10. Flashing: Shall be provided at all roof-wall intersections, windows, doors, chimneys, decks, balconies and 
other areas as necessary to prevent water from entering behind the Aggre-flex System and 
wall system.

1.05 PERFORMANCE REQUIREMENTS
A. Aggre-flex System shall have been tested as follows:
EIFS Weather Resistance and Durability Performance*
	TEST
	METHOD
	CRITERIA
	RESULTS

	1. Accelerated Weathering
	ASTM G153

(Formerly ASTM G23)
	No deleterious effects at 2000 hours when viewed under 5x magnification
	Pass 

	2. Accelerated Weathering
	ASTM G154 (Formerly ASTM G53) 
	No deleterious effects at 2000 hours 
	Pass

	3. Freeze/Thaw Resistance
	ASTM E2485
	No deleterious effects at 10 cycles when viewed under 5x magnification
	Pass

	4. Water Penetration
	ASTM E331 (modified per ICC-ES AC 235)
	No water penetration beyond the plane of the base coat/insulation board interface after 15 minutes at 6.24 psf (299 Pa) or 20% of design wind pressure, whichever is greater
	Pass at 2.86 psf (137 Pa), 6.24 psf (299 Pa), and 12.0 psf (575 Pa) consecutively

	5. Water Resistance
	ASTM D2247
	No deleterious effects at 14 day exposure
	Pass @ 28 days

	6. Salt Spray
	ASTM B117
	No deleterious effects* at 300 hours
	Pass @ 300 hrs

	7. Abrasion Resistance
	ASTM D968
	No cracking or loss of film integrity at 528 quarts (500 L) of sand
	Pass 

	8. Mildew 
   Resistance
	ASTM D3273
	No growth supported during 28 day exposure period
	Pass 

	9. Impact 
   Resistance
	ASTM E2486
	Level 1: 25-49 in-lbs (2.83-5.54J)

Level 2: 50-89 in-lbs (5.65-10.1J)

Level 3: 90-150 in-lbs (10.2-17J)

Level 4: >150 in-lbs (>17J)
	Pass with one layer Standard Mesh

Pass with one layer Standard Mesh

Pass with Medium & Standard Mesh
Pass with Strong & Standard Mesh

	10. Transverse Wind Load
	ASTM E330
	Withstand positive and negative wind loads as specified by the building code.
	Pass.  Assemblies vary from 68-287 psf*


* Ultimate wind loads – contact Master Wall for specific assemblies.
EIFS Fire Performance
	TEST
	METHOD
	CRITERIA
	RESULT

	1. Fire Endurance
	ASTM E119
	Maintain fire resistance of existing rated assembly
	See Technical Bulletin MW#168-030111 for assemblies

	2. Radiant Heat Ignition
	NFPA 268


	No ignition @ 20 minutes
	Pass 

	3. Surface Burning
 (individual 
  components)
	ASTM E84
	Individual components shall each have a flame spread of 25 or less, and smoke developed of 450 or less
	Flame Spread: 0
Smoke Developed: 0


EIFS Component Performance
	TEST
	METHOD
	CRITERIA
	RESULT

	1. Alkali Resistance of Reinforcing Mesh
	ASTM E2098 (formerly EIMA 105.01)
	Greater than 120 pli (21 dN/cm) retained tensile strength 
	Pass

	2. Requirements for Rigid PVC Accessories
	ASTM D1784
	Meets cell classification 13244C
	Pass

	EPS (Physical Properties)
Thermal Resistance

Flame Spread

Smoke Developed
	ASTM C303, D1622

ASTM C272

ASTM E84
	4.0 @ 4.4 °C (40 °F)

3.6 @ 23.9 °C (75 °F)
25 max.

450 max.


	Pass

Pass

Pass


1.06 QUALITY ASSURANCE

A. Qualifications

1. System Manufacturer: Shall be Master Wall Inc.®.  All materials shall be manufactured or sold by Master 
Wall Inc.® and shall be purchased from Master Wall Inc.® or its authorized distributors.

2. Contractor: Shall be knowledgeable in the proper installation of the Master Wall Inc.® Aggre-flex 
System and shall be experienced and competent in the installation of Exterior Insulation and Finish 
Systems.  Additionally, the contractor shall possess a current Master Wall Inc.® applicator certificate 
issued by Master Wall Inc.®
3. Insulation Board Manufacturer: Shall be approved by Master Wall Inc.®, shall be capable of producing the 
Expanded Polystyrene (EPS) in accordance with current Master Wall Inc.® specification and code 
requirements and have a third party quality assurance program in place.

B. Regulatory Requirements

1. The EPS shall be separated from the interior of the building by a minimum 15-minute thermal barrier.

2. The use and maximum thickness of EPS shall be in accordance with the applicable building codes.

C. Certification

1. The Aggre-flex System shall be recognized for the intended use by the applicable building 
code(s).

D. Mock-Up

1. The contractor shall, before the project commences, provide the owner/architect with a mock-up for 
approval.

2. The mock-up shall be of suitable size as required to accurately represent the products being installed, as 
well as each color and texture to be utilized on the project.

3. The mock-up shall be prepared with the same products, tools, equipment and techniques required for the 
actual application.  The finish used shall be from the same batch that is being used on the project.

4. The approved mock-up shall be available and maintained at the job site.

5. For panelized construction, the mock-up shall be available and maintained at the panel fabrication location.

1.07 DELIVERY, STORAGE AND HANDLING

A. All Master Wall Inc.® materials shall be delivered to the job site in the original, unopened packages with labels 
intact.

B. Upon arrival, materials shall be inspected for physical damage, freezing, or overheating.  Questionable 
materials shall not be used.

C. Deliver all materials in original unopened packages with labels intact. Verify all quantities, colors, and textures 
against bill of lading.

D. Store all materials protected from direct exposure to weather conditions and at temperatures not less than 40°F 
(4°C) or greater than 110°F (43°C).

E. Stack insulation board flat, fully supported off the ground and protected from direct exposure to the sun.

F. Material Safety Data Sheets (MSDS) or Safety Data Sheets (SDS) shall be supplied for the components of the 
EIFS and be available at the job site.

1.08 PROJECT CONDITIONS

A. Ambient air temperatures shall be 40°F (4°C) or greater and rising at the time of installation of the Master Wall 
Inc.® products and shall remain at 40°F (4°C) or greater for at least 24 hours after application.

B. Provide supplemental heat and protection as required when the temperature and conditions are not in 
accordance with installation requirements. Sufficient ventilation and time shall be provided to ensure that 
materials have sufficiently dried prior to removing supplemental heat.

C. Adequate protection shall be provided to prevent weather conditions (humidity, temperature, and precipitation) 
from having an affect on the curing or drying time of Master Wall Inc.® materials.

D. Adjacent materials and the Aggre-flex System shall be protected during installation and while curing 
from weather and shall be protected from site damage.

E. Coordinate installation of the Aggre-flex System with related work specified in other sections to 
ensure that the wall assembly is protected to prevent water from getting behind the system. The cap flashing 
shall be installed as soon as possible after the finish coat has been applied. When this is not possible, 
temporary protection shall be provided immediately in this area.

F. All sealant work shall be installed in a timely manner. Protect open joints from water intrusion during 
construction with backer rod, or temporary covering, until permanently sealed.

G. Sufficient manpower and equipment shall be employed to ensure a continuous operation, free of cold joints, 
scaffolding lines, and texture variations, etc.

H. Existing Conditions - The contractor shall have access to electric power, clean water, and a clean work area at 
the location where the Master Wall Inc.® materials are to be applied.

1.09 SEQUENCING AND SCHEDULING

A. Installation of the Aggre-flex System shall be coordinated with other construction trades.

B. Sufficient manpower and equipment shall be employed to ensure a continuous operation, free of cold joints, 
scaffold lines, texture variations, etc.

1.10 LIMITED MATERIALS WARRANTY

A. Provide a manufacturer’s warranty against defective material upon request.  

 1.11 MAINTENANCE

A. Maintenance and repair shall follow the procedures noted in Master Wall Inc.® Technical Bulletins #112 and 
#129.

PART II – PRODUCTS

2.01 MANUFACTURER

A. All components of the Aggre-flex System shall be supplied or obtained from Master Wall Inc.® or its 
authorized distributors.  Substitutions or additions of materials other than specified will void the warranty.

2.02 MATERIALS
A. Portland Cement: Shall be Type I or II, meeting ASTM C 150, white or gray in color, fresh and free of lumps.

B. Water: Shall be potable, clean and free of foreign matter.

C. Metal Flashing Components:  Complying with SMACNA Recommendations.  Reference Section 07620. 

D. Sealant Systems: Reference Sealant Specification, Section 07900.

E. Window & Door Systems:  Detailed by the designer and suitable for EIFS.  Reference Section 08000.

2.03 COMPONENTS

(Typical Application/Optional Component)

A. Starter Tracks/Casing
1. Vinyl Corp. foundation sill screed product #WS50-250U, Plastic Components Product # 632-50, Amico 
Foundation Weep Screed AMFWS425-500, Amico Foundation Weep Screed (NO. 7) or approved equal.

2. Vinyl Corp. PB Starter Strip/Casing Bead product # CBS 150-16W or Plastic Components Starter Trac 
product # STWP-15 shall be used in accordance with Master Wall Inc.® details. 

3. Alternate termination methods may be used in accordance with Master Wall Inc.® details and 
recommendations.

B. Mechanical Fasteners and Plastic Washers


1.  The Wind-Devil 2 plate or approved equal shall be used with the appropriate corrosion-resistant fastener 

shall be used to meet the requirements of the specific project, local building code and the anticipated wind 

loads.
C. Adhesives


1. Master Wall Inc. Foam & Mesh (F&M) Adhesive: An acrylic-based product mixed one-to-one by weight with 

Portland cement designed for use with reinforcing mesh as the base coating over the insulation board.


2. Master Wall Bagged Base Coat (MBB): A polymer based cementitious product mixed with 5 to 6 quarts of 

water for use as an adhesive and base coating over the insulation board.


3. F&M Plus: An acrylic-based high build product mixed one-to-one by weight with Portland cement designed 

for use with reinforcing mesh as the base coating over the insulation board. (This product shall be used 

where indicated on the construction drawings when a leveling base coat is required.)


4. Expanded PolyStyrene Adhesive (EPSA): a water-based acrylic copolymer adhesive formulated to bond 

MEPS insulation board to plywood and other approved substrates.

D. Insulation Board

1. Insulation Board shall meet or exceed ASTM C-578.

2. Nominal 1.0 pcf, aged expanded polystyrene.

3. Flamespread and smoke development shall be 25 and 450 or less respectively per ASTM E-84.

4. Maximum size 2’x4’x4” (.61 m x 1.22 m x 102 mm). Refer to actual contract documents to determine actual 
insulation board thickness.

E. Reinforcing Mesh

Open weave glass fiber fabric, treated for alkaline resistance and compatibility with Master Wall Base Coats, 
and conforming ASTM D-76, D-579, D-5035, MIL-Y-1140 and meeting a minimum Medium Impact 
Resistance (50-89 in-lbs) when tested to EIMA 101.86 Impact Resistance Standards.
1. Detail Mesh 

2. Standard Mesh 

3. Hi-Tech Mesh 

4. Medium Mesh 

5. Strong Mesh 

6. Ultra Mesh 

F. Base Coats

1. Master Wall Inc.® Foam & Mesh (F&M) Adhesive: An acrylic-based product mixed one-to-one by weight 
with Portland cement for use with reinforcing mesh as the base coating over the insulation board.

2. Master Wall Bagged Base Coat (MBB): A polymer based cementitious product mixed with 5 to 6 quarts of 
water for use with reinforcing mesh as the base coating over the insulation board.
3. F&M Plus: An acrylic-based high build product mixed one-to-one by weight with Portland cement designed 
for use with reinforcing mesh as the base coating over the insulation board. (This product shall be used 
where indicated on the construction drawings when a leveling base coat is required.)


4. Expanded Polystyrene Base (EPSB): a 100% pure acrylic polymer based noncementitious base coat.

G. Water Resistant Adhesive & Base Coat 

1.  Guardian – An acrylic-based product mixed one-to-one by weight with Portland cement for use as the 
adhesive to bond insulation board to an approved substrate and/or as a base coat with reinforcing mesh 
over insulation board. (This product should be used as designated on the construction drawings where 
additional resistance to moisture is needed.)

H. Primer – Especially useful under dark colors
1. Primecoat Primer - Acrylic-based tintable primer

2. Sanded Primecoat Primer - Acrylic-based tintable primer with sand

I. Superior Finishes: Master Wall Inc.® Superior Finishes are acrylic-based wall coatings available in a variety of 
colors and textures. The following textures are available:

1. Perfect2.0 (Perfect) - riled texture

2. Fine Sand 1.0 (Spray) – sand type texture

3. Medium Sand 1.5 (Desert Sand) – coarse sand texture

5. Versatex 0.5 (Refinish) – Fine texture used to create numerous finishes

J. Finish Enhancements
1. Silicone Coat - Factory added silicone enhancement for better water resistance and to keep buildings 
cleaner.

2. Excel Mildew Enhancement - Factory added mildew booster exceeding ASTM D3273 requirements.

3. Elastomeric Plus - Increases flexibility and bridges minor hairline cracks.

K. Specialty Finishes
1. Superior Stone

2. Aggrestone

3. Lumia

4. Plaster Flex

5. Metallic Cote

6. Savannah

7. Marbleflex

8. Travertine

9. Eco Glass

10 Aggrelime

11. Brick Finish System

L. Accents & Coatings
1. Roller-flex architectural coating

2. Elasto-flex elastomeric architectural coating

3. Clearshield clear protective coating

4. Vintique antiquing accent

PART III – EXECUTION

3.01 EXAMINATION

A. Prior to installation of the Aggre-flex System, the contractor shall verify that the substrate:

1. Is of a type listed in Section 1.04.C.1.

2. Is flat within 6.4 mm (1/4 in) in a 3 m (10 ft) radius.

3. Is sound, dry, connections are tight, has no surface voids, projections or other conditions that may interfere 
with the Aggre-flex System installation or performance.

B. Prior to the installation of the Aggre-flex System, the architect or general contractor shall insure that all needed 
flashings and other waterproofing details have been completed, if such completion is required prior to the 
Aggre-flex application.  Additionally, the Contractor shall ensure that:

1. Metal roof flashing has been installed in accordance with Asphalt Roofing Manufacturers Association 
(ARMA) Standards.

2. Openings are flashed in accordance with the Aggre-flex System Installation Details or as otherwise 
necessary to prevent water penetration.

3. Chimneys, Balconies, and Decks have been properly flashed.

4. Windows, Doors, etc. are installed and flashed per manufacturer's requirements and the Aggre-flex 
System Installation Details.

C. Prior to the installation of the Aggre-flex System, the contractor shall notify the general contractor, and/or 
architect, and/or owner of all discrepancies.

3.02 PREPARATION

A. Aggre-flex materials shall be protected by permanent or temporary means from inclement weather 
and other 
sources of damage prior to, during, and following application until completely dry.

B. Protect adjoining work and property during Aggre-flex installation. 

C. The substrate shall be prepared as to be free of foreign materials, such as, oil, dust, dirt, form release agents, 
efflorescence, paint, wax, water repellents, moisture, frost and any other condition that inhibit adhesion.

3.03 GENERAL GUIDELINES

A. The system shall be installed in accordance with the current Master Wall Inc.® Aggre-flex System 
Application 
Instructions.

B. The overall minimum base coat thickness shall be sufficient to fully embed the mesh.  

C. Sealant shall not be applied directly to textured finishes.

D. When installing the Aggre-flex System, adhere according to Master Wall Inc.® and local requirements.

3.04 AGGRE-FLEX EIFS INSTALLATION

A. Design Considerations

1. The minimum slope of inclined surfaces shall not be less than 6” (152 mm) in 12” with a maximum length of 
12” unless approved in writing by Master Wall Inc.®. Inclined surfaces which are or could be defined as 
roofs by the building codes or application are not approved by Master Wall Inc.®
2. The use of dark colors must be considered in relation to wall surface temperature as a function of local 
climatic conditions.

3. The Insulation Board shall be separated from the interior of the building by a 15-minute thermal barrier.

4. The use and maximum thickness of insulation board shall be in accordance with the applicable building 
codes, typically ¾” (19 mm) minimum and 4” (102 mm) maximum.

5. The EIF System shall be recognized by a current code report.

6. It is the responsibility of the architect and the purchaser to determine if a product is suitable for their 
intended use. The architect or designer of the project shall be responsible for all decisions pertaining to the 
design, details, structural capability, attachment details, shop drawings and the like. Master Wall Inc.® has 
prepared specifications, details and data sheets to assist as guidelines for the use and installation of the 
products. Master Wall Inc.® is not responsible for the design, details, structural capability, attachment 
details and shop drawings whether it is based on Master Wall Inc.® information or not.

7. Expansion joints in the system are required at building expansion joints, at prefabricated panel joints, where 
substrates change, at floor lines in wood framed construction, and where structural movement is 
anticipated.  Reference construction documents for exact locations.


8. Aesthetic Joints may be installed to provide sufficient break points in the EIF System to prevent cold joints 

from occurring in the finish coat. Aesthetic joints shall not be used in lieu of an expansion joint
B. Mixing                                                                                                                       

1. Mix the products following the instructions on the product data sheets.

2. Additives shall not be added to Master Wall Inc.® materials unless written approval has been received from 
Master Wall Inc.® 

C. Preparation                                                                                                               

1. Protect contiguous work from damage during application of the Aggre-flex EIF System. Temporary covering 
may be required to prevent over spray or splattering of exterior finish coatings on other work.

2. Protect substrate from inclement weather during installation. Prevent infiltration of moisture behind the 
system that may affect the substrate or the attachment of the insulation board to the substrate.

3. Adhesive, Base Coats and Finishes shall not be installed when ambient air temperature is below 40ºF (4ºC). 
The temperature shall remain at or above 40ºF (4ºC) during mixing, application and until materials have 
cured.

4. Sufficient scaffolding, manpower and tools shall be provided to prevent cold joints.

5. Flashings shall be installed as required by construction documents and Master Wall Inc.® details in a 
manner to prevent the intrusion of water behind the insulation board and wall system. All flashing materials 
should direct the water to the exterior face of the finished system.

D. Installation, General                                                                                     

1. Reference architectural details for full wall system requirements.

2. Comply with the manufacturers’ current published instructions, (specifications, details, data sheets and 
technical bulletins) for the installation of the Aggre-flex EIF System.

3. Comply with local building codes.

4. Verify that all flashings and other items are in place.

E. Starter Track or Casing Option

1. Install the starter track, casing or alternate termination method where the system ends at the foundation.  
Install track at least 6” (152 mm) above grade, at least ¾” (19 mm) above structurally supported 
paving/patios, or at least 2” (51 mm) above unsupported patios
2. Backwrap details are used in accordance with Master Wall Inc.® details.

3. Alternatively, casing beads can be installed at other areas such as around window and door openings.  

F. Backwrapping 

1. Adhesively or mechanically secure reinforcing detail or standard mesh to the substrate positioned so that a 
minimum of 2 ½” (63.5 mm) of the mesh is onto the substrate. (The reinforcing mesh shall be wide enough 
to encapsulate the edge of the insulation board and cover both the substrate and the face of the insulation 
board a minimum of 2 ½”.)

2. After the insulation board is applied, complete the backwrapping procedure by applying the base coat, 
embedding the remaining mesh and returning it onto the face of the insulation board.

3. Where sealants are applied the reinforcing mesh color shall not be visible and the texture of the base coat 
shall be smooth so that the pattern of the mesh is covered.

4. Apply finish in accordance with manufacturer’s details. (Finish shall not be applied to areas where the 
design professional has anticipated dynamic movement or at an EIFS to EIFS joint.).

3.05 FIELD QUALITY CONTROL

A. The contractor shall be responsible for the proper application of the Aggre-flex materials.

B. Master Wall Inc.® assumes no responsibility for on-site inspections or application of its products.

C. If required, the contractor shall certify in writing the quality of work performed relative to the substrate system, 
details, installation procedures, workmanship and as to the specific products used.

D. If required, the EPS supplier shall certify in writing that the EPS meets Master Wall Inc.® specifications.

E. If required, the sealant contractor shall certify in writing that the sealant application is in accordance with the 
sealant manufacturer’s and Master Wall Inc.® recommendations.
F. Master Wall Inc.’s current published details, specifications, data sheets, technical bulletins and other 
literature/information are minimum standards and guidelines that shall be followed when designing and 
detailing a project with the Aggre-flex EIF System.

G.
Details shall conform to Master Wall Inc.’s details and shall be consistent with the project requirements.

H.
Master Wall Inc. must approve deviations from the standard published details in writing.

I.
The architect, engineer or the designer of the project should determine where the dew point would occur in 

relationship to the wall assembly and the project location during summer and winter conditions.

J.
Drip details shall be specified in accordance with Master Wall Inc.’s published details.

K.
At all locations the reinforced base coat, trim accessories or the substrate shall encapsulate the approved 

insulation board.

3.06 INSULATION APPLICATION               
A. Insulation Application - Adhered                                                                            

1. Notched Trowel Method - Foam & Mesh (F& M) Adhesive, Master Wall Bagged Base Coat (MBB), F&M 
Plus shall be applied to the entire surface of one face of the approved insulation board.

2. Apply the adhesive mixture directly to the back of the insulation board using approved stainless steel 
notched trowel.  With the trowel at a 45 degree angle, cover the entire back of the insulation board with full 
beads of adhesive.  Apply the adhesive so the ribbons run vertically when applied to the wall. 

3. Do not adhere the edges of the insulation board to each other.

4. Apply the approved insulation board over a dry substrate with the long edge oriented horizontally.

5. The application of the insulation board shall commence at the base of the wall from a level line of support.

6. After the adhesive has been applied to insulation board it shall be installed by sliding it into place until it 
abuts adjoining insulation board.

7. Uniform pressure shall be applied over the entire surface of the insulation board to achieve contact with the 
substrate. Periodically check the contact of the adhesive to the substrate by removing a piece of insulation 
board. Proper adhesive contact should be demonstrated by the evidence of similar amounts of adhesive 
adhered to both the insulation board and the substrate. The cohesive break should occur when the board 
is removed. If the cohesive break had occurred prior to the adhesive set the substrate is more than likely 
out of plane and should be corrected to meet minimum standards of this specification. If a cohesive failure 
does not occur contact a Master Wall representative.

8. The insulation board shall be installed in a running bond pattern with staggered vertical joints.

9. Insulation boards shall be interlocked at the inside and outside corners.

10. Insulation board joints shall be offset from the sheathing joints a minimum of 6” (152 mm).

11. Insulation board joints shall be offset from the corners of openings.

12. Allow for proper spacing at windows, doors, penetrations and other openings so that sealant systems can 
be installed in accordance with Master Wall Inc.® specification, details and the construction documents.

13. Provide a proper joint through insulation board where expansion joints occur in substrates and where 
required in the system.

14. Wrap mesh in or around details in accordance with Master Wall Inc.® instructions.

15. The insulation board shall be butted tightly. Any gaps greater than 1/16” (1.6 mm) between insulation 
boards shall be filled with slivers of insulation board. Adhesive shall not be used to adhere foam when 
filling gaps.

16. Gaps between insulation boards shall not be filled with adhesive or base coat materials.

17. Allow adhered insulation to remain undisturbed for a period of 12 hours prior to rasping the foam.
B.
Insulation Application - Mechanically Attached


1. Fasten the insulation board using Wind-lock Wind-Devil 2 or approved washer and appropriate 
corrosion-

resistant fastener.  Master Wall Inc. must approve other mechanical fastening systems in writing prior to 

use with the Aggre-flex System.


2. Fastening patterns shall be determined by the requirements of the geographical conditions of the area, local 

code requirements and the performance of the fasteners, washers and their test results in conjunction with 

the 
specified substrate and the thickness of foam specified for use.

C.
Apply the approved insulation board over a dry substrate with the long edge oriented horizontally.

D.
The application of the insulation board shall commence at the base of the wall from a level line of support at 
the casing bead or termination.

E.
The insulation board shall be installed in a running bond pattern with staggered vertical joints.

F.
Insulation boards shall be interlocked at the inside and outside corners.

G.
Insulation board joints shall be offset from the sheathing joints a minimum of 6” (152 mm).

H.
Insulation board joints shall be offset from the corners of openings.

I.
Allow for proper spacing at windows, doors, penetrations and other openings so that sealant systems can be 
installed in accordance with Master Wall Inc.’s specification, details and the construction documents.

J.
Provide a proper joint through insulation board where expansion joints occur in substrates and where required 
in the system.

K.
Wrap mesh in or around details in accordance with Master Wall Inc. instructions.

L.
The insulation board shall be butted tightly. Any gaps greater than 1/16” (1.6 mm) between insulation boards 
shall be filled with slivers of insulation board. Adhesive shall not be used to adhere foam when filling gaps.

M.
Gaps between insulation boards shall not be filled with adhesive or base coat materials.

N.
Rasp the entire surface of the insulation board to level any irregularities. All irregularities greater than 1/16” 
(1.6 mm) shall be sanded flat.

O.
Cut aesthetic joints as indicated on construction drawings. Always maintain a minimum ¾” (19 mm) of 
insulation board under aesthetic joints.

P.
Spot fasteners with base coat and allow to dry.

Q.
Clean rasped insulation board in preparation for base coat application.

3.07 BASE COAT APPLICATION  
A. Base Coat Preparation

1. Inspect adhered insulation board to ensure the installation meets the requirements set forth in Master Wall 
Inc.® specification, details, data sheets, technical bulletins and the construction documents. Make 
necessary repairs to ensure the installation meets the requirements prior to commencement of the base 
coat application.

2. Fill any gaps in the insulation board with slivers of insulation.

3. Rasp the insulation board to provide a true surface within specifications.  If the foam is yellowed or has 
developed a powdery film due to sun exposure the foam must be rasped and cleaned prior to the base 
coat application.

4. Complete the backwrapping at all system terminations by embedding the reinforcing mesh as described in 
Section 3.06 of this specification.

5. Install minimum 9 ½” x 12” (229x309 mm) diagonal reinforcement at all windows, doors, louvers, or other 
penetration corners. Apply field mesh as soon as possible after diagonal mesh application.

6. Reference architectural documents for locations of designed impact classifications.

B. Base Coat Application

1. Apply the base coat to the entire surface of the insulation board to the thickness required for the specified 
reinforcing mesh to be applied in a given area.

a. Standard, Detail and Hi-Tech Mesh require a nominal 1/16” (1.6 mm).


b. Medium, Strong and Ultra Mesh requires a nominal 3/32” (2.4 mm).
2. Immediately embed Master Wall Inc.® reinforcing mesh into wet base coat with a trowel, working from the 
center toward the edges, until the mesh is fully covered and a smooth surface is achieved. The color of the 
mesh shall not be visible but a slight mesh pattern may be visible.

3. Lap mesh 2 ½” (64 mm) minimum on all sides. (Do not lap Strong or Ultra mesh.)

4. Reinforcing Mesh shall be continuous through all interior and exterior corners extending beyond the corner 
a minimum of 12” from both directions creating a minimum of two layers of standard reinforcing mesh on 
all interior and exterior corners.

5. Standard and Hi-Tech reinforcing mesh can be applied in a single layer.

6. Medium Mesh can be applied in one layer yet it may require an additional coat of base coat mixture to 
properly embed the mesh after the first coat has dried.

7. Strong and Ultra Mesh require a second layer of base coat reinforced with Standard or Hi-Tech Mesh.

8. EPS shapes shall have reinforcing mesh embedded into the base coat.

9. Allow the base coat to cure a minimum of 12 hours prior to additional base coat or finish coat applications.

3.08 FINISH COAT APPLICATION  
A. Superior Finish Coat Application

1. Surface irregularities in the base coat, such as trowel marks, insulation board lines and reinforcing mesh 
laps shall be corrected prior to the finish application.

2. Apply the Master Wall Inc.® Superior Finish in the color and texture as approved by the project owner or the 
project architect with sufficient manpower and equipment to insure a continuous operation without cold 
joints, scaffolding lines etc. Texture finish shall match approved jobsite samples. Thickness and coverage 
will vary depending on the specified final appearance.

3. Trowel Application – (Perfect 2.0, Fine Sand 1.0, Medium Sand 1.5, Versatex 0.5)

a. Apply the Superior Finish to the clean, dry and cured base coat with a stainless steel trowel.

b. Level the surface to a uniform thickness of 3/32” to 1/8” (2.4-3.2 mm).

c. Float the Finish with a plastic float in a uniform motion to achieve the desired texture. (Versatex 0.5 
cannot be floated easily. A second application of the Versatex 0.5 may be applied to create the 
desired texture.)

4. Spray Application – (Perfect 2.0, Fine Sand 1.0, Medium Sand 1.5, Versatex 0.5)

a. Prime surface with Master Wall Inc.® Primecoat or Sanded Primecoat tinted to match the selected finish 
color. Allow Primecoat or Roller-Flex to cure a minimum of 12 hours prior to finish coat application.

b. Using a conventional plaster hopper gun or a proven pump, spray finish over the primed base coat to 
achieve desired texture using a circular overlapping pattern keeping the spray gun at a 90º angle to 
the surface and maintaining the same distance to the wall at all times.

c. Be cautious of flooding an area with too much finish because it may appear shinier when it dries.

5. Specialty Finishes:  Follow individual product data sheet application instructions.

3.09 JOB SITE CLEANUP

A.
Clean work area in accordance with contract documents removing all excess materials, droppings and debris. 
Clean adjacent surfaces.

B.
Other trades may now install their work – Sheet Metal (Section 07620), Sealants (Section 07900), Mechanical 
(Section 15000), Electrical (Section 16000).

3.10 PROTECTION


A. Aggre-flex System shall be protected from inclement weather and other sources of damage until dry and 


permanent protection in the form of flashings, sealants, etc. are installed.

Disclaimer

This Specification is published for general informational purposes only and is not intended to imply that these are the only materials, procedures, or methods, which are available or suitable. Materials, procedures, or methods may vary according to the particular circumstances, local building code requirements, design conditions, or statutory and regulatory requirements. While the information in this specification is believed to be accurate and reliable, it is presented without guarantee or responsibility on the part of Master Wall Inc.®
�





Master Wall Inc.®


PO Box 397


Fortson, GA 31808


706-569-0092


800-755-0825


www.masterwall.com








Master Wall Guide Specification AF
Issued: 1/1/16

Page 13 of 13

